- PROCEDURE FOR TUBE PRODUCTION

- Seamless Tube Production.

| Flow | Activity | Responsibility | Ref |
| --- | --- | --- | --- |
| RECEIVING MATERIAL | - Examine production plan - Check compound received for quantity and quality (Laboratory approval) - Check other material received from stores | SPM/SAPM/Pro Ex/SUP ,, ,, | PC-PLAN 02 IT-FORM-02 PC-PLAN-02 IFS |
| STRAIN EXTRUDER | - Carryout strain extrusion | OPERATOR | TU-WI-001 |
| TUBE EXTRUSION | - Masticate sieved compound in mill - Maintain milling conditions. - Maintain extrusion conditions. - Valve applying / Gum applying - Cut tube to required length with tolerance for shrinkage. - Load trolley and let stand for shrink completely. | OPERATOR ,, ,, ,, ,, ,, | TU-WI-001 ,, ,, TU-WI-001/ 007 TU-WI-001 ,, |
| SPLICING | - Sizing to the required length - Splice green tube and joint ends. - Traceability no punching - Stock in splicing trolleys | OPERATOR ,, ,, ,, | TU-WI-002/003 ,, TU-WI-008 TU-WI-002/003 |
| SAMPLING INSPECTION TESTING | - Cure 01 no selected tube by representing each lot - Check joint strength. (1st test) - If the strength is satisfactory, continue the production process - If the joint strength is not satisfactory, set splicer setting and re – Check (2nd test /3rd test) If the test results are satisfactory, continue the production process If the test result are negative, green tubes are subjected to recycling - Issue IMI form for compound problems | O/SUP ,, SPM/SAPM/Pro Ex/SUP ,, ,, ,, ,, | TU-WI-004 TU-WI-009 ,, ,, ,, ,, |
| Flow | Activity | Responsibility | Ref |
| AUTO VULCANIZING & COUSTOMER BASED TEST | - Place spliced green tube on a tray. - Vulcanize using chamber. - Test pull strength. | OPERATOR ,, ,, | TU-WI-004 ,, TU-WI-009 |
| MOULDING | - Place green tube on pre-forming mould and inflate. - Vulcanize tube inside under steam or air pressure. | OPERATOR ,, | TU-WI-004 ,, |
| HANDING OVER | - Send tubes to grading section for tube grading and final inspection | SPM/SAPM/Pro Ex/SUP | TU-WI-004/015 IFS |

- Un assemble tube production& Joint Preparation

| Flow | Activity | Responsibility | Ref |
| --- | --- | --- | --- |
| PLANNING | - Examine the production | SPM/SAPM/Pro Ex/SUP | PC-PLAN-02 |
| RECEIVING MATERIAL | - Check rubber compound received for: - Quantity - Quality (Laboratory approval) - Check other material received from the stores | SPM/SAPM/Pro Ex/SUP ,, | PC-PLAN-02 IFS PC-PLAN-02 IFS |
| STRAIN EXTRUSION | - Carryout compound in mill | OPERATOR | TU-WI-001 |
| TUBE EXTRUSION | - Masticate sieved compound in mill - Maintain milling conditions. - Maintain extrusion conditions. - Cut tube to required length with a tolerance for shrinkage. - Load to trays and let stand to shrink completely | OPERATOR ,, ,, ,, ,, | TU-WI-001 ,, ,, ,, ,, |
| MANDREL LING, VULCANIZING, DE- MANDRELLING | - Insert tube to the mandrel - Remove the air between tube and mandrel - Vulcanize in chamber - Remove tube from mandrel | OPERATOR ,, ,, ,, | TU-WI-014 ,, ,, ,, |

| Flow | Activity | Responsibility | Ref |
| --- | --- | --- | --- |
| ASSEMBLY | - Carryout assembling | OPERATOR | TU-WI-013 |
| VULCANIZING | - Apply solvent at joint - Press hand roller to remove creases & trapped air bubbles. - Vulcanize joint in joint press machine - Check press stations. - Record test results. - Remove vulcanized tube and keep in box with relevant details | OPERATOR ,, ,, ,, ,, ,, | TU-WI-013 ,, TU-WI-013 ,, TU-WI-013 |
| SAMPLING, DESTRUCTIVE & NON DESTRUCTIVE TEST | - Collect sample - Carryout non destructive test - Record test results - Carryout destructive test - Record test results. | O/PA/SUP ,, ,, ,, ,, | TU-WI-009 ,, ,, ,, ,, |
| ACCEPTANCE | - If the test results are satisfactory approve the process - If the test results are not satisfactory Keep the lot under ”ON HOLD” Collect sample 2nd test. Test results are 100% satisfactory, approved the lot if not reject | SPM/PE/APM /Pro Ex/PA/ SUP ,, | TU-WI-009 |
| HANDING OVER | - Send tubes to grading section for tube grading and final inspection | SPM/Pro Ex/ PA/ SUP/O | TU-WI-013/015 IFS |